### Hallowell®

### High-Capacity Reinforced Bolted Shelving Specification

Finishing:  All shelving components to be cleaned and coated after fabrication with a seven stage zinc/iron phosphate solution to inhibit corrosion, followed by a coat of high grade custom blend powder electrostatically sprayed and baked at 350 degrees Fahrenheit for a minimum of 20 minutes to provide a tough durable finish.

Color for all steel components: Shall be 725 Dark Gray.

Shelving shall be GREENGUARD Gold CertificationSM

Angle Post: Shall be 2" x 2" x 13 gauge cold rolled steel corner post uprights punched on 1” centers.

Reinforced Shelves: Fabricated from 14 gauge cold rolled steel and double flanged at all four sides.  An 18 gauge hat channel shape stiffener is welded to the underside of the shelf running left to right increasing capacity and preventing deflection under heavy loading.  All four corners are punched to allow shelves to be securely bolted to angle posts. Minimum four nuts and bolts per corner.

One-Year Warranty:  HALLOWELL shelving is covered against all defects in materials and workmanship excluding finish, damage resulting from deliberate destruction and vandalism under this section for a period of one year.